## Slide 1: Surface Roughness and Tool Wear Prediction Sayantika Ghosh M.Tech Smart Manufacturing

## Slide 2: Surface Roughness Prediction in Turning Using Three Artificial Intelligence Techniques; A Comparative Study [1]
In this work vibration signals collected during the turning process of steel rods at different cutting conditions were processed and analysed using three AI techniques to predict the class of surface roughness (smooth, medium and rough surface finish).
Results:
Differential Evolution algorithm performed better than particle swarm optimization and genetic algorithm.
Feed rate plays a dominant role in determining surface roughness and it generally increases with increasing feed rate.
Accuracy of 80% was obtained in the best case.
Research Gaps Identified:
Relationship between the cutting parameters (except the feed rate) and the surface roughness was not explicitly mentioned.
Can be extended to acoustic signals along with the vibration signals.
Features can be combined to obtain more features which can help in increasing the overall accuracy.

## Slide 3: Investigation Of Surface Roughness In Turning of In-situ Al6061- TiC Metal Matrix Composite By Taguchi And Prediction Of Response by ANN [2]
In the present investigation, the effect of surface roughness in turning of in-situ developed Al6061-10 Wt% TiC metal matrix composite rod was studied in dry cutting condition by applying Taguchi technique and ANOVA and finally an ANN model was developed to predict the surface roughness.
Results:
S/N ratio showed that the optimal surface roughness value was obtained at higher cutting speeds and lower feed rate and depth of cut.
From ANOVA and regression analysis it was found that highest contribution comes from cutting speed followed by feed rate and depth of cut. (ANOVA ---> cutting speed - 43%, feed rate - 31% and depth of cut - 26%)
From p values it was found that all the three process parameters were significant.
Average percentage error was 1.51 so ANN could be used further to predict surface roughness.
Novelty of the paper:
New material (Al-TiC metal matrix composites) was used here.
Research Gaps Identified:
From ANOVA result it was found that cutting speed had the highest contribution followed by feed rate but there are papers in the literature which states that feed rate have the highest influence on the surface roughness.
Different ANN architecture might be tried to improve the overall accuracy.

## Slide 4: Application Of Regression And Artificial Neural Network Analysis In Modelling Of Surface Roughness In Hard Turning Of AISI 52100 Steel [3]
The aim of this present study is to analyze the effects of cutting parameters such as cutting speed, feed rate and depth of cut on surface roughness and to predict the values of surface roughness by developing RA and ANN models during turning of AISI 52100 steel in dry machining condition.
Results:
Prediction capability of ANN model was better than the RA model presented in this work with the best ANN architecture being 3-6-6-1.
From ANOVA result, it was observed that the feed rate is the most significant parameter among the factors considered. The percent contribution of each factor on the measured surface roughness is as follows: feed rate factors (83.15%), cutting speed factors (9.52%) and depth of cut factors (5.12%).
Optimal surface roughness was obtained at higher value of cutting speed and lower value of feed rate and depth of cut.
Research Gaps Identified:
Here feed rate was the most dominant factor which is different from the result obtained in paper 2.

## Slide 5: Influencing factors and theoretical modeling methods of surface roughness in turning process: State-of-the-art [4]
A systematic review of influencing factors and theoretical modeling methods of surface roughness in turning process are analyzed in the present work with its advantages, disadvantages and challenges.
Results:
Feed rate has a more pronounced influence on surface roughness than the other two factors, i.e. the cutting velocity and cutting depth.
Feed rate showed non-linear behaviour and the relation between tool tip cannot be understood.
Influencing factors of surface roughness were classified into the ‘easy’ modeling factors and ‘difficult’ modeling factors.
Research Gaps Identified:
Difficult modeling factors can be further divided based on their influencing modes- certain and uncertain factors.
The influential factors (tool wear) for the established models of surface roughness is in the spatial dimension but they are not investigated in the time domain. Therefore, the effects of influencing factors in time dimension on turned surface roughness should be further investigated.

## Slide 6: Evaluation of turned and milled surfaces roughness using convolutional neural network [5]
This study proposes the use of convolutional neural network to predict the arithmetic average value of roughness profile (Ra) and the average height of the roughness profile (Rz) by analysing the pattern of ridges and valleys in the digital image of surface textures.
Results:
Other loss functions used here (MAE, MAPE, log-cosh, Huber) outperformed the standard MSE because the machine image dataset did not show gaussian distribution.
The models with MAPE loss function achieved the highest accuracy as it is less susceptible to outlier data.
The average error of Ra, Rz prediction using the best model is verified to be within 10% of the actual measured surface roughness values.
The experiment results indicate the computational time for estimation is within the desired range, thus confirming the method’s practicability to be applied for in-between process roughness evaluations.
Novelty of the paper:
Existing computer vision techniques to measure surface roughness rely on feature extraction which is a complicated process requiring complicated setups, long prediction time, requiring high computational and expert decisions in selecting appropriate surface features. So this study proposes the use of convolutional neural network to evaluate the surface roughness directly from the array of image of surface textures as the input of the algorithm.
Research Gaps Identified:
The proposed evaluation models using CNN took relatively longer training time than other vision-based prediction methods. To address this issue, developing an adaptive model which can automatically adjust hyperparameters value based on its real time performance during the training process could be considered in future studies.

## Slide 7: Surface roughness modeling in high speed turning of Ti-6Al-4V – Artificial Neural Network approach [6]
This study deals with the modeling of surface roughness parameters Ra and Rt by considering machining parameters like cutting speed, feed rate and depth of cut along with uncontrollable parameters like tool flank wear and cutting tool vibrations in high speed dry turning of Ti-6Al-4V alloy.
Results:
SW-ELM outperformed with its prediction accuracy, MSE and execution time when compared to MLP and RBFNN. SW-ELM prediction accuracy was 100% on both Ra and Rt, with a MSE of 0.00683 in case of Ra whereas 0.004837 for Rt for 30 hidden neurons and least execution time when compared to MLP and RBFNN.
SW-ELM gave the highest prediction accuracy with maximum number of hidden neurons making the model less compact.
MLPNN on the other hand generated compact network with least number of hidden neurons.
Novelty of the paper:
New model like SW-ELM was used for the prediction of surface roughness in titanium alloy and uncontrollable parameters like tool wear and cutting tool vibration were used.

## Slide 8: Surface roughness diagnosis in hard turning using acoustic signals and support vector machine: A PCA-based approach [7]
To monitor the surface quality during the cycle without interrupting the machining process and to establish the relation between audible sound emitted during process and the resulted surface finish.
Results:
A correlation does exist between the surface roughness and the sound energy.
Could identify three different levels of surface roughness achieving an average accuracy of 100.00%.
RBF kernel has a better performance when compared to the Linear one, while the multi-class classification approach has not affected the system accuracy.
Novelty of the paper:
The use of sound has not been explored for surface roughness diagnosis with the PCA dimensionality reduction, and that makes it the major contribution of this work.
Research Gaps Identified:
Evaluate the influence of noise coming from other machines, or even from the environment in this process
To test the proposed method for monitoring tool usage, wear.

## Slide 9: Prediction of surface roughness in hard turning under high pressure coolant using Artificial Neural Network [8]
The aim of the present work is to employ artificial neural network to develop a model to predict average surface roughness parameter in hard turning of steels.
Results:
The 3-10-1 and 3-4-2 ANN models, trained by Bayesian Regularization, revealed the lowest RMSE.
Two possible solutions were advised: (a) use of 3-10-1 for only high pressure coolant assisted turning but not for dry turning, (b) use of 3-4-2 for both dry and HPC applied turning. In addition, using ‘3-n-2’ provides less setup time with acceptable accuracy.
Preferable cutting parameters are - higher cutting speed, lower feed rate, lower to moderate hardness of material, and lastly application of HPC .
Novelty of the paper:
Development of models for high pressure coolant assisted turning, besides dry cutting;
Inclusion of material hardness as input;
Neural network based model wherein all possible architectures were used;
Determination of the effect of hidden neuron number on the prediction accuracy;
Selection of the best training algorithm from Levenberg–Marquardt (LM), Bayesian Regularization (BR) and Scaled Conjugate Gradient (SCG) algorithms which makes the work accurate and more reliable from other presented works.
Research Gaps Identified:
Other prediction models could be tried further.

## Slide 10: In-process prediction of surface roughness in turning of Ti–6Al–4V alloy using cutting parameters and vibration signals [9]
In this work, an attempt has been made to use only vibration signals for in-process prediction of surface roughness during turning of Ti–6Al–4V alloy. If only vibration signals were not able to provide good prediction then to select a set of significant cutting parameters and vibration signals to predict surface roughness with sufficient accuracy using multiple regression and artificial neural network technique.
Results:
This model provided good prediction accuracy (maximum percentage error 7.45%) of surface roughness.
Prediction accuracy for the model having considered only the vibration signal is not that great so in order to improve the accuracy included the cutting parameters along with the vibration signal.
It is evident that cutting speed and acceleration amplitude of vibration in axial direction are weakly related with surface roughness as the correlation coefficient is close to zero.
Pearson correlation coefficient for feed rate was maximum followed by acceleration amplitude of vibration in radial direction, depth of cut and acceleration amplitude of vibration in tangential direction
Novelty of the paper:
An effort has been made in this work to determine whether the cutting parameters can be completely replaced by vibration signals to predict the surface roughness. From the fundamental concepts of design of experiment, it follows that in Box Behnken Design of Response Surface Methodology, use of vibration signals to predict the surface roughness is not possible as the vibrations cannot be directly controlled to serve as independent variables.
Research Gaps Identified:
Accuracy of the prediction model could be improved further.

## Slide 11: Investigation of signal behaviors for sensor fusion with tool condition monitoring system in turning [10]
First, the relationship between sensor signals and tool wear has been investigated. Secondly, the sensor signal behaviors at the moment of tool breakage were observed. Lastly, the effects of cutting parameters on averaged values of VB were examined.
Results:
Temperature and AE signals were compatible with each other and demonstrated good correlation (74%) between tool wear.
Cutting force components demonstrate weak correlation with VB (27% for FT and FF, 19% for FR).
Dynamically fluctuating of AE signals during entire turning refer to the minor tool breakage, irregular chip formation and fracture namely deterioration of cutting geometry and possible tool breakage. Accelerometer and current sensor also provide reliable information for tool breakage.
The increase in feed rate and cutting speed enhances VB values
Novelty of the paper:
This was the first time in indirect TCM, five different sensors were adopted to a lathe for collecting data to measure the capability of each sensor in reflecting the tool wear.
Research Gaps Identified:
Other tool wear types and surface roughness parameters could be analysed.

## Slide 12: Tool condition monitoring during hard turning of AISI 52100 Steel: A case study [11]
This paper deals with an online monitoring of flank wear and roughness of turned surface while turning of AISI 52100 hardened bearing steel by means of multilayer carbide insert (coated) under dry condition considering process parameters and vibration signals.
Results:
From the main effect plot, cutting speed is predominant factor for tool flank wear, surface roughness and acceleration amplitude of vibration.
Result data indicates that the highest acceleration amplitude of vibration (0.924 m/s2) noticed with highest speed combination whereas lowest acceleration (0.316 m/s2 ) is noticed with lowest speed combination. Higher values of feed are more prominent to produce higher surface roughness. Highest tool wear achieved at highest speed 150 m/min whereas lowest wear noticed at lowest speed 70 m/min. Chipping of tool or breakage of tooltip are noticed at highest speed (150 mm/min), lowest feed (0.04 mm/rev) and moderate depth of cut (0.2 mm) but mostly abrasion were observed.
Process parameters such as depth of cut, cutting speed and vibration signals (d,v,Vy) have strong correlations with the flank wear as Pearson correlation coefficients are positive except feed (f) as it is negative.
Similarly, for surface roughness, acceleration amplitude (0.599), cutting speed (0.357) and feed (0.65) have strong correlation except for depth of cut as it yields negative value and referred as weak correlations.
Prediction models through linear regression are significant as its P-values are less than 0.05 and accuracy of the predictions have been improved significantly.
It has been observed that the value of machining time depends on the cutting conditions [15], i.e. values for Vc, f and d. Once more cutting speed and feed are predominant, depth of the cut seems to less influent.
Research Gaps Identified:
Only linear regression was considered

## Slide 13: Condition monitoring of turning process using infrared thermography technique – An experimental approach [12]
In the present work, a real time process monitoring method of the tool condition was explored using multiple sensors in turning of AISI 316L steel by using both coated and uncoated carbide inserts.
Results:
While cutting speed and feed rate proved to be influential parameter on the depicted temperatures and depth of cut was the least influential parameter.
Generally, it is observed that lower heat and temperatures are generated when coated inserts are employed. It is found that cutting temperatures are gradually increased as edge wear and deformation developed.
Novelty of the paper:
The design of tool condition monitoring system for reduced complexity and increased robustness has been rarely studied. Therefore, present work concentrates on design of effective multi sensor-based TCM with reduced complexity while machining AISI 316L steel using both coated and uncoated inserts.

## Slide 14: Real Time Tool Wear Condition Monitoring in Hard Turning of Inconel 718 Using Sensor Fusion System [13]
To introduce a sensor based tool wear monitoring system for hard turning of Inconel718 material consisting of a vibration sensor and a force based measurement system.
Results:
The study shows that force data is quite useful to establish a strong correlation between the cutting force and tool wear.
Statistical ANOVA results showed that speed is influencing the most with 73.3% contribution, followed by depth of cut with 25.4% contribution, while feed has negligible effect on the tool wear.
Tool wear rate increases with time. Three distinct phases of tool wear namely initial wear, gradual wear and rapid wear are observed during machining.
It was observed that only vibration in general shows the non-linear trend with the actual tool wear. It can predict only tool wear state and not the actual tool wear values because of its non-linearity. So in order to model the vibration parameters, advanced approaches like artificial neural network, genetic algorithm and/or fuzzy logic etc. or some other approach like force data acquisition in combination with vibrations is to be used for establishing the relation between tool wear and vibration signal.
Novelty of the paper:
This study uses more than one sensor which is advantageous since the loss of sensitivity in one sensor domain can be offset by information from the other sensor ensuring more accurate and reliable results. Hence, on-line tool monitoring system with sensor fusion system can be used effectively to estimate the state of tool in real time more accurately and reliably.
Research Gaps Identified:
More sensors can be added with existing dual sensing method to ensure the highest accuracy in online tool wear monitoring system.

## Slide 15: References
Abu-Mahfouz I, Rahman AE, Banerjee A. Surface Roughness Prediction in Turning Using Three Artificial Intelligence Techniques; A Comparative Study. Procedia Computer Science. 2018; 140:258–267. Available from: https://doi.org/10.1016/j.procs.2018.10.322
Kishore DSC, Rao KP, Basha SMJ, Rao BJP. Investigation Of Surface Roughness In Turning of In-situ Al6061- TiC Metal Matrix Composite By Taguchi And Prediction Of Response by ANN. Materials Today: Proceedings. 2018; 5:18070–18079.
Paturi UMR, Devarasetti H, Narala SKR.Application Of Regression And Artificial Neural Network Analysis In Modelling Of Surface Roughness In Hard Turning Of AISI 52100 Steel. Materials Today: Proceedings. 2018; 5:4766–4777.
He CL, Zong WJ, Zhang JJ. Influencing factors and theoretical modeling methods of surface roughness in turning process: State-of-the-art. International Journal of Machine Tools and Manufacture. 2018; 129: 15-26. Available from: https://doi.org/10.1016/j.ijmachtools.2018.02.001 .
Rifai AP, Aoyama H, Tho NH, Dawal SZM, Masruroh NA. Evaluation of turned and milled surfaces roughness using convolutional neural network. Measurement. 2020; 161: 107860. Available from: https://doi.org/10.1016/j.measurement.2020.107860.
D’Mello G, P. SP, Shetty RP. Surface roughness modeling in high speed turning of Ti-6Al-4V – Artificial Neural Network approach. Materials Today: Proceedings. 2017; 4:7654–7664.
Papandrea PJ, Frigieri EP, Maia PR, Oliveira LG, Paiva AP. Surface roughness diagnosis in hard turning using acoustic signals and support vector machine: A PCA-based approach. Applied Acoustics. 2020; 159:107102. Available from: https://doi.org/10.1016/j.apacoust.2019.107102 .
Mia M, Dhar NR. Prediction of surface roughness in hard turning under high pressure coolant using Artificial Neural Network. 2016; 92: 464-474. Available from: http://dx.doi.org/10.1016/j.measurement.2016.06.048 .
Upadhyay V, Jain PK, Mehta NK. In-process prediction of surface roughness in turning of Ti–6Al–4V alloy using cutting parameters and vibration signals. Measurement. 2013; 46: 154-160. Available from: http://dx.doi.org/10.1016/j.measurement.2012.06.002
Kuntoglu M, Saglam H. Investigation of signal behaviors for sensor fusion with tool condition monitoring system in turning. Measurement. 2020; 108582. Available from: https://doi.org/10.1016/j.measurement.2020.108582 .
Panda A, Sahoo AK, Panigrahi I, Kumar R. Tool condition monitoring during hard turning of AISI 52100 Steel: A case study. Materials Today: Proceedings. 2018; 5: 18585-18592.
Prasad BS, Prabha KA, Kumar PVSG. Condition monitoring of turning process using infrared thermography technique – An experimental approach . Infrared Physics & Technology. 2017; 81: 137-147. Available from: http://dx.doi.org/10.1016/j.infrared.2016.12.023 .
Mali R, Telsang MT, Gupta TVK. Real Time Tool Wear Condition Monitoring in Hard Turning of Inconel 718 Using Sensor Fusion System. Materials Today: Proceedings. 2017; 4: 8605-8612.